7/24/13

COMPACTION REQUIREMENTS

Project No.  XXXXXX          C.N.  XXXX

Project Name:

The following compaction requirements are recommended for the plans.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

COMPACTION REQUIREMENTS

Class III (See Specifications)

|  | SOIL TYPE | DEPTH BELOW FINISH SUBGRADE | PERCENT DENSITY | MOISTURE REQUIREMENTS |
| --- | --- | --- | --- | --- |
|  |  |  |  | MINIMUM | MAXIMUM |
| Embankment / Roadway Grading, including driveways, to receive concrete pavement | Silt-Clay | Upper 3 feet | 98 Min. | Opt. -3% | Opt. +2% |
|  | Silt-Clay | At depths greater than 3 feet | 95 Min. | Opt. -3% | Opt. +2% |
|  | Granular | All depths | 100 Min. | ** | ** |
| Embankment / Roadway Grading, including driveways, to receive flexible pavement | Silt-Clay | Upper 3 feet | 100 Min. | Opt. -2% | Opt. +1% |
|  | Silt-Clay | At depths greater than 3 feet | 95 Min. | Opt. -3% | Opt. +2% |
|  | Granular | All depths | 100 Min. | ** | ** |
| Embankment / Roadway Grading not to be surfaced | All | All depths | 95 Min. | Opt. -3% | Opt. +2% |
| _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ |
| Subgrade Preparation, Shoulder Subgrade Preparation (Concrete Pavement) | Silt-Clay | The upper 6 inches of subgrade soil | 98 Min. | Opt. -3% | Opt. +2% |
|  | Granular | The upper 6 inches of subgrade soil | 100 Min. | ** | ** |
| Subgrade Preparation, Shoulder Subgrade Preparation (Flexible Pavement) | Silt-Clay | The upper 6 inches of subgrade soil | 100 Min. | Opt. -2% | Opt. +1% |
|  | Granular | The upper 6 inches of subgrade soil | 100 Min. | ** | ** |
| _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ |
| Embankment of driveways which are not to be surfaced | All | All depths | Class I | (See Specifications) |
| Bituminous Pavement Patching | All | Underlying Material | 100 Min. | (See Specifications) |
| Foundation Course / Subgrade Stabilization | - - | - - | 100 Min. | (See Specifications) |
| Stabilized Subgrade (ie Lime, Flyash, etc.) | - - | - - | 100 Min. | (See Special Provisions) |
| Trench Widening | - - | - - | 100 Min. | (See Special Provisions) |
| _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ _ |
| Granular Structural Fill (MSE Walls, Granular Fill for bridges, Culverts, etc) | Granular | All depths | 100 Min. | Opt. -3% | Opt. +3% |
| ** Moisture as necessary to obtain density. (A moisture target value at maximum density shall be established in the field by the Contractor during the compaction process. The acceptable moisture content shall be ± 2% of the target value.) * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * |